API 5CT STANDARD
Standard :API SPEC 5CT、APISPEC 5B、ISO11960
Tubing is used to extracting petroleum and natural gas from a well.
Casting serves as walls of a well
Size of Tubing
	Size
	Weight Designation
	Outside Diameter
	Wall Thickness
	Type of End Finish
	

	
	
	
	
	Grade
	

	Designation
	T&C Non－Upset
	T&C Extemal Up set
	In
	Mm
	In
	Mm
	J55
	L80-1
	N80
	C90
	T95
	P110
	

	1.9
	2.4
	　
	1.9
	48.26
	0.125
	3.18
	PI
	　
	　
	　
	　
	　
	

	
	
	
	
	
	
	
	
	
	
	
	
	
	

	
	2.75
	2.9
	1.9
	48.26
	0.145
	3.68
	PNUI
	PNUI
	PNUI
	PNUI
	PNUI
	PNUI
	

	
	3.65
	　
	1.9
	48.26
	0.2
	5.08
	PU
	PU
	PU
	PU
	PU
	PU
	

	2.3/8
	4
	　
	2.375
	60.32
	0.137
	4.24
	PN
	PN
	PN
	PN
	PN
	　
	

	
	4
	4.7
	2.375
	60.32
	0.19
	4.83
	PNU
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	5.8
	5.95
	2.375
	60.32
	0.254
	6.45
	　
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	6.6
	　
	2.375
	60.32
	0.259
	7.49
	　
	P
	　
	P
	P
	　
	

	
	7.35
	　
	2.375
	60.32
	0.336
	8.53
	　
	PU
	　
	PU
	PU
	　
	

	2.7/8
	6.4
	6.5
	2.875
	73.02
	0.217
	5.51
	PNU
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	7.8
	7.9
	2.875
	73.02
	0.276
	7.01
	　
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	8.6
	8.7
	2.875
	73.02
	0.308
	7.82
	　
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	9.35
	9.45
	2.875
	73.02
	0.34
	8.64
	　
	PU
	　
	PU
	PU
	　
	

	
	10.5
	　
	2.875
	73.02
	0.392
	9.96
	　
	P
	　
	P
	P
	　
	

	
	11.5
	　
	2.875
	73.02
	0.44
	11.18
	　
	P
	　
	P
	P
	　
	

	3.1/2
	7.7
	　
	3.5
	88.9
	0.216
	5.49
	PN
	PN
	PN
	PN
	PN
	　
	

	
	9.2
	9.3
	3.5
	88.9
	0.254
	6.45
	PNU
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	10.2
	　
	3.5
	88.9
	0.289
	7.34
	PN
	PN
	PN
	PN
	PN
	　
	

	
	12.7
	12.95
	3.5
	88.9
	0.375
	9.52
	　
	PNU
	PNU
	PNU
	PNU
	PNU
	

	
	14.3
	　
	3.5
	88.9
	0.43
	10.92
	　
	P
	　
	P
	P
	　
	

	
	15.5
	　
	3.5
	88.9
	0.476
	12
	　
	P
	　
	P
	P
	　
	

	
	17
	　
	3.5
	88.9
	0.53
	13.46
	　
	P
	　
	P
	P
	　
	

	4
	9.5
	　
	4
	101.6
	0.226
	5.74
	PN
	PN
	PN
	PN
	PN
	　
	

	
	10.7
	11
	4
	101.6
	0.262
	6.65
	PU
	PU
	PU
	PU
	PU
	　
	

	4.1/2
	12.6
	12.75
	4.5
	114.3
	0.271
	6.88
	PNU
	PNU
	PNU
	PNU
	PNU
	　
	

	
	15.2
	　
	4.5
	114.3
	0.337
	8.56
	　
	P
	　
	P
	P
	　
	

	
	17
	　
	4.5
	114.3
	0.38
	9.65
	　
	P
	　
	P
	P
	　
	

	
	18.9
	　
	4.5
	114.3
	0.43
	10.92
	　
	P
	　
	P
	P
	　
	

	
	21.5
	　
	4.5
	114.3
	0.5
	12.7
	　
	P
	　
	P
	P
	　
	

	
	23.7
	　
	4.5
	114.3
	0.56
	14.22
	　
	P
	　
	P
	P
	　
	

	
	26.1
	　
	4.5
	114.3
	0.63
	16
	　
	P
	　
	P
	P
	　
	



































	Weight
Designation
	Outside Diameter
	Wall Thickness
	Type of End Finish?? Grade

	
	in
	mm
	in
	mm
	J55K55
	L80-1
	N80
	C90
	C95
	T95
	P110
	M65

	9.5
	4.5
	114.3
	0.205
	5.21
	PS
	　
	　
	　
	　
	　
	　
	　

	10.5
	4.5
	114.3
	0.224
	5.69
	PSB
	　
	　
	　
	　
	　
	　
	　

	11.6
	4.5
	114.3
	0.25
	6.35
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	13.5
	4.5
	114.3
	0.29
	7.37
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	15.1
	4.5
	114.3
	0.337
	8.56
	　
	　
	　
	　
	　
	　
	PLB
	　

	11.5
	5
	127
	0.22
	5.59
	PS
	　
	　
	　
	　
	　
	　
	　

	13
	5
	127
	0.253
	6.43
	PSLB
	　
	　
	　
	　
	　
	　
	　

	15
	5
	127
	0.296
	7.52
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	18
	5
	127
	0.362
	9.19
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	21.4
	5
	127
	0.437
	11.1
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	23.2
	5
	127
	0.478
	12.14
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	24.1
	5
	127
	0.5
	12.7
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	14
	5.5
	139.7
	0.244
	6.2
	PS
	　
	　
	　
	　
	　
	　
	　

	15.5
	5.5
	139.7
	0.275
	6.99
	PSLB
	　
	　
	　
	　
	　
	　
	　

	17
	5.5
	139.7
	0.304
	7.72
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	20
	5.5
	139.7
	0.361
	9.17
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	23
	5.5
	139.7
	0.415
	10.54
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	26.8
	5.5
	139.7
	0.5
	12.7
	　
	　
	　
	P
	　
	P
	　
	　

	29.7
	5.5
	139.7
	0.562
	14.27
	　
	　
	　
	P
	　
	P
	　
	　

	32.6
	5.5
	139.7
	0.625
	15.88
	　
	　
	　
	P
	　
	P
	　
	　

	35.3
	5.5
	139.7
	0.687
	17.45
	　
	　
	　
	P
	　
	P
	　
	　

	385
	5.5
	139.7
	0.75
	19.05
	　
	　
	　
	P
	　
	P
	　
	　

	40.5
	5.5
	139.7
	0.812
	20.62
	　
	　
	　
	P
	　
	P
	　
	　

	43.1
	5.5
	139.7
	0.875
	22.22
	　
	　
	　
	P
	　
	P
	　
	　

	20
	6.625
	168.28
	0.288
	7.32
	PSLB
	　
	　
	　
	　
	　
	　
	　

	24
	6.625
	168.28
	0.352
	8.94
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	28
	6.625
	168.28
	0.417
	10.59
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	32
	6.625
	168.28
	0.475
	12.06
	　
	PSLB
	PSLB
	PSLB
	PSLB
	PSLB
	PSLB
	PSLB

	20
	7
	177.8
	0.272
	6.91
	PS
	　
	　
	　
	　
	　
	　
	　

	23
	7
	177.8
	0.317
	8.05
	PSLB
	PLB
	PLB
	PLB
	PLB
	　
	　
	PLB

	26
	7
	177.8
	0.362
	9.19
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	29
	7
	177.8
	0.408
	10.36
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	32
	7
	177.8
	0.453
	11.51
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	35
	7
	177.8
	0.498
	12.65
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	38
	7
	177.8
	0.54
	3.72
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	26.4
	7.625
	193.68
	0.328
	8.33
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	　

	29.7
	7.625
	193.68
	0.375
	9.52
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	33.7
	7.625
	193.68
	0.43
	10.92
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	39
	7.625
	193.68
	0.5
	12.7
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	42.8
	7.625
	193.68
	0.562
	14.27
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	45.3
	7.625
	193.68
	0.595
	15.11
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	47.1
	7.625
	193.68
	0.625
	15.88
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	24
	8.625
	219.08
	0.264
	6.71
	PS
	　
	　
	　
	　
	　
	　
	　

	28
	8.625
	219.08
	0.304
	7.72
	　
	　
	　
	　
	　
	　
	　
	　

	32
	8.625
	219.08
	0.352
	8.94
	PSLB
	　
	　
	　
	　
	　
	　
	　

	36
	8.625
	219.08
	0.4
	10.16
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	　

	40
	8.625
	219.08
	0.45
	11.43
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	44
	8.625
	219.08
	0.5
	12.7
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	49
	8.625
	219.08
	0.557
	14.15
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	32.3
	9.625
	244.48
	0.312
	7.92
	　
	　
	　
	　
	　
	　
	　
	　

	36
	9.625
	244.48
	0.352
	8.94
	PSLB
	　
	　
	　
	　
	　
	　
	PSLB

	40
	9.625
	244.48
	0.395
	10.03
	PSLB
	PLB
	PLB
	PLB
	PLB
	PLB
	　
	PSLB

	43.5
	9.625
	244.48
	0.435
	11.05
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	47
	9.625
	244.48
	0.472
	11.99
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB

	53.5
	9.625
	244.48
	0.545
	13.84
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	　

	58.4
	9.625
	244.48
	0.595
	15.11
	　
	PLB
	PLB
	PLB
	PLB
	PLB
	PLB
	　

	59.4
	9.625
	244.48
	0.609
	15.47
	　
	　
	　
	P
	　
	P
	　
	　

	64.9
	9.625
	244.48
	0.672
	17.07
	　
	　
	　
	P
	　
	P
	　
	　

	70.3
	9.625
	244.48
	0.734
	18.64
	　
	　
	　
	P
	　
	P
	　
	　

	75.6
	9.625
	244.48
	0.797
	20.24
	　
	　
	　
	P
	　
	P
	　
	　

	32.75
	10.75
	273.5
	0.279
	7.09
	　
	　
	　
	　
	　
	　
	　
	　

	40.5
	10.75
	273.5
	0.35
	8.89
	PSB
	　
	　
	　
	　
	　
	　
	PSB

	45.5
	10.75
	273.5
	0.4
	10.16
	PSB
	　
	　
	　
	　
	　
	　
	PSB

	51
	10.75
	273.5
	0.45
	11.43
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB

	55.5
	10.75
	273.5
	0.495
	12.57
	　
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB

	60.7
	10.75
	273.5
	0.545
	13.84
	　
	　
	　
	PSB
	　
	PSB
	PSB
	　

	65.7
	10.75
	273.5
	0.595
	15.11
	　
	　
	　
	PSB
	　
	PSB
	PSB
	　

	73.2
	10.75
	273.5
	0.672
	17.07
	　
	　
	　
	P
	　
	P
	　
	　

	79.2
	10.75
	273.5
	0.734
	18.64
	　
	　
	　
	P
	　
	P
	　
	　

	85.3
	10.75
	273.5
	0.797
	20.24
	　
	　
	　
	P
	　
	P
	　
	　

	42
	11.75
	298.45
	0.333
	8.46
	　
	　
	　
	　
	　
	　
	　
	　

	47
	11.75
	298.45
	0.375
	9.53
	PSB
	　
	　
	　
	　
	　
	　
	PSB

	54
	11.75
	298.45
	0.435
	11.05
	PSB
	　
	　
	　
	　
	　
	　
	PSB

	60
	11.75
	298.45
	0.489
	12.42
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB

	65
	11.75
	298.45
	0.534
	13.56
	　
	P
	P
	P
	P
	P
	P
	　

	71
	11.75
	298.45
	0.582
	14.78
	　
	P
	P
	P
	P
	P
	P
	　

	48
	13.375
	339.72
	0.33
	8.38
	　
	　
	　
	　
	　
	　
	　
	　

	54.5
	13.375
	339.72
	0.38
	9.65
	PSB
	　
	　
	　
	　
	　
	　
	PSB

	61
	13.375
	339.72
	0.43
	10.92
	PSB
	　
	　
	　
	　
	　
	　
	PSB

	68
	13.375
	339.72
	0.48
	12.19
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB

	72
	13.375
	339.72
	0.514
	13.06
	　
	PSB
	PSB
	PSB
	PSB
	PSB
	PSB
	　

	65
	16
	406.4
	0.375
	　
	　
	　
	　
	　
	　
	　
	　
	　

	75
	16
	407.4
	0.438
	PSB
	　
	　
	　
	　
	　
	　
	　
	PSB

	84
	16
	408.4
	0.495
	PSB
	　
	　
	　
	　
	　
	　
	　
	PSB

	109
	16
	409.4
	0.66
	PSB
	P
	P
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